ECP 555 SILVER PLATED COPPER

EMI/RFI SHIELDING COATING

DESCRIPTION

ECP 555 Silver/ Copper aerosol combines the EMI shielding properties with a convenient method of application for prototype and touch-up work, it is designed to give low resistance, in thin film thickness, displaying excellent adhesion to most plastics it is ideal for electronic equipment housing. It exhibits excellent long term shielding and grounding properties while providing an aesthetically pleasing appearance.

PHYSICAL PROPERTIES

Surface resistance at 25 micron

thou) ASTM D257					0.7 ohm/square or less

Pigment					Silver plated copper

Flash Point					- 5C

Typical coverage					approx 6 square feet.

TYPICAL PROPERTIES

Sheet resistance 		<0.1 /square at 25 m

Attenuation		 75 dB at 50 m

Maximum service temperature 	95C

DIRECTIONS FOR USE

Surface preparation:  All contaminants including mould release, grease and dirt must be removed.  Mask areas that do not require spraying.

Mixing:  Shake vigorously for a minimum of 2 minutes to evenly distribute contents.

Spray a small area to check compatibility with substrate.

Application:  Operate in an upright position, spraying in light, even strokes from side to side to avoid flooding.  Shake briefly at intervals during spraying.  On completion, invert the

aerosol and spray to clear valve and nozzle.  It is advised to clear any excess material

from the nozzle at frequent intervals to prevent blockage.  If the nozzle blocks, use a pin

to clear the opening, or remove the nozzle and flush with Toluene, Xylene or MEK.

Replace the nozzle taking care to point the opening away from you.

PRECAUTIONS:

Pressurised container.  Protect from sunlight and do not expose to temperature exceeding 50 deg C.  Do not pierce or burn, even after use.  Do not spray on an open flame or any incandescent material.  Keep away from sources of ignition - No smoking .

Consult health and safety data before use.

Drying

ECP 555 is touch dry in approx. 5 minutes and to handle in about 10 minutes, depending on ambient temperature and film thickness. Best results will be seen 4 to 16 hour's air drying (dependant upon film thickness and ambient temperature). It can be force dried for 20 minutes at 60C after a short flash off time.

Quality Control

Measure the surface resistance after coating is fully dried. Digital ohmmeter measurements using the same type of fixed test probe rigs avoids confusion and is highly recommended, although corner to corner readings are also frequently used.

Cleaning

Masks can be easily cleaned with solvent. Overspray can be removed from plastics with 40/60% acetone/IPA wipe.

The data sheet relates to material as supplied.

the information contained herein is given in good faith , but no liability will be accepted by the company in relation to the same. the acquisition of additional information may necessitate revisions to part or all of the data sheet, and such information will be supplied when it becomes available

as the company's products are used for a multiplicity, of purposes, and as the company has no control over the method of their application or use, the company excludes all warranties, expressed or implied, by statue or other  otherwise, as to their products and or their fitness in any particular purpose.

any technical co-operation between our company and the customer is given for the customers assistance only and without liability on the part of  the company.